| Technical Results |  |  |  |  |
| --- | --- | --- | --- | --- |
| Description | Hard and durable fine-grained tight-texture limestone |  |  |  |
| Country of Origin | UK |  |  |  |
| Geological Type | Magnesium limestone |  |  |  |
| Colour | White |  |  |  |
| Density | 2140 kg/m³ |  | BSEN 1936 |  |
| Compressive Strength | 81.8 MPa |  | EN 722-1 |  |
| Compressive Strength | 90.7 MPa (56 cycles) after freeze thaw |  | EN 722-1 |  |
| Water Absorption at atmospheric pressure | 9.3% by mass |  | BSEN 13755 |  |
| Water Absorption by Capillarity | 67.5 |  | EN 722-11 |  |
| Open Porosity | 23.6% |  | BS EN 1936 |  |
| Slip Resistance | 79 Dry 79 Wet |  | BSEN 14231 |  |
| Abrasion Resistance | 24.5mm |  | BS EN 14151 |  |
| Flexural Strength under conc. load: | 7.5 MPa perpendicular to bed 5.1 MPa (56 Cycles) perpendicular after freeze thaw |  | BSEN 12372 BSEN 12372 |  |
| Flexural Strength under conc. Load: | 8.6 MPa parallel to bed 9.9 MPa (14 Cycles) parallel to bed after freeze thaw 7.7 MPa (20 Cycles) parallel to bed after thermal shock |  | BSEN 12372 BSEN 12372 BSEN 12372 |  |
| Breaking load at Dowel hole | 2350 N |  | BSEN 13364 |  |
| Design thermal conductivity | 1.7W (m.k)-1 |  | EN 12524 |  |
| Specific Heat capacity | 1000 J/(Kg. K) |  | EN 12524 |  |
| Water vapour resistance factor: | Dry 200 Wet 150 |  | EN12524 |  |
| Average Block Size | 1500L x 1000W x 600H |  |  |  |

Please note that stone is a natural product and all results are subject to variation

Cadeby Beds 11-13

Sales:

Block Stone Limited

Grant House

Prospect Way

Hutton

CM13 1XD

Tel: +44 (0) 1246 554450

Email: sales@blockstone.com

www.blockstone.com

Quarry Location:

Cadeby Quarry

Garden Lane

Doncaster

South Yorkshire, England